For further information, please contact:

Samantha Joubert, Marketing Communications Coordinator, South Africa.

Tel: +27 11 821 3602    / Fax: +27 (0) 86 681 4342

# Samantha.joubert@skf.com

For Immediate Publication

12 May 2017

SKF delivers higher-performance across its INSOCOAT bearings range

With its latest generation of electrically insulated bearings, SKF has raised the performance standard to provide constant electrical performance, even in high humidity.

SKF’s INSOCOAT bearings range comprises bearings with an electrically insulating coating on the external surfaces of its inner or outer ring, plasma-sprayed with an aluminium oxide coating. The coating, which is naturally hygroscopic, is sealed with a resin to protect against the conductive effects of high humidity and moisture ingress.

These bearings are specially designed and manufactured for use in rotating electrical machines, such as industrial electric motors, traction motors and generators. They prevent the passage of harmful electrical currents from the rotor to the machine frame via the bearings, which causes progressive electrical erosion of the bearings’ rolling contact surfaces and ultimately premature failure.

Following the introduction of an improved plasma spray coating process and optimised ceramic layer, SKF can provide this superior insulating coating as standard and off-the-shelf across its entire INSOCOAT range.

INSOCOAT bearings are now able to withstand voltages of 3000V DC sufficient to cope with the vast majority of stray bearing current problems in electrical machines.

2/...INSOCOAT bearings

2/...INSOCOAT bearings

In addition, the upgraded moisture-resistant coating provides greater protection against humidity storage environments which can compromise a bearing’s insulating properties before it is even placed in service, making INSOCOAT bearings highly robust during transport and handling.

Combining both bearing and insulation in a single solution, INSOCOAT protects against electrical erosion at significantly lower total cost of ownership compared with other techniques such as shaft or housing insulation.

## SKF is a leading global supplier of bearings, seals, mechatronics, lubrication systems, and services which include technical support, maintenance and reliability services, engineering consulting and training. SKF is represented in more than 130 countries and has around 17,000 distributor locations worldwide. Annual sales in 2015 were SEK 75 997 million and the number of employees was 46 635. www.skf.com

## ® SKF is a registered trademark of the SKF Group.
™ BeyondZero is a trademark of the SKF Group.

By: 		Sonia Laverick

Laverick Media Communications cc

Tel: +27 (0) 11 0400 818

sonia@laverickmedia.co.za / www.laverickmedia.co.za